# Proof of delivery

REGUPOL Germany GmbH & Co. KG

Am Hilgenacker 24

57319 Bad Berleburg

+49 2751 803-0

commercial@regupol.de www.commercial.regupol.com

| Position | Quantity |  | Scope of work |  | Unit price |  | Total price |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | m² |  | Subfloor preparation The substrate prepared for installation must comply with the requirements of the applicable national standards. Attention must be paid to VOB Part C – DIN 18365 as well as the increased requirements for finished floor surfaces according to DIN 18202, Table 3, Line 4. Furthermore, all EN and DIN standards recognized at the time of execution, as well as the generally accepted rules of trade and state of the art, shall apply. | €/m² |  | € |  |
| 2 | m² |  | REGUPOL upscale® 4 mm heterogeneous resilient commercial floor covering. Supply and installation. Design: LRP® Dimensions: 1.200 x 230 x 4 mm Including beveled edge Material: EPDM granules and PUR binder, factory sealed. Performance fleece backing to facilitate easier deinstallation. Thickness (EN ISO 24346): 4 mm. Weight (EN ISO 23997) approx. 4.0 kg/m². Reaction to Fire (EN 13501-1): Cfl-s1. Slip Resistance (EN 16165, Annex B): R10. Impact Sound Reduction (EN ISO 10140): 14 dB. VOC emissions: Assessment according to AgBB 2021 — requirements fulfilled. CE marking according to EN 14041 — information to follow. The floor covering must be installed in accordance with the installation guidelines of both the adhesive manufacturer and the flooring manufacturer. | €/m² |  | € |  |
| 3 |  | lm | Baseboards: The use of adhesive insert baseboards is recommended. This solution creates a seamless visual transition from the floor covering onto the wall. Cut stripes from the specified flooring to match the required width of the self-adhesive baseboard and insert them accordingly. Install the baseboard on the wall properly and in accordance with standard industry practices. |  | €/lm |  | € |  |

Total: €